TOTAL: 4 PAGES (INCL. THIS ONE)

Document Number：                　　　　　　　　　　　　　　　　　     Revision：3

Document Title：Product Specification of Ni-MH  ESP13000FH Cell                       Page 1of  3

1、 SCOPE

This specification governs the performance of the following Nickel-Metal hydride Cylindrical cell and its    stack-up battery。

Model：ESP13000FH

Cell Size：F平(φ32.3±0.2×89.0±0.5)

F尖(φ32.3±0.2×90.5±0.5)

2 、DATA OF STACK UP BATTERIES

All data involves voltage and weight to stack-up battery are equal to the value of unit cell time the number of   unit cell which consisted in the stack-up batteries

Example ：Stack-up batteries consisting three unit cells

Nominal voltage of unit cell=1.2V

Nominal voltage of stack-up batteries =1.2V×3=3.6V

- RATINGS

| Description | Unit | Specification | Conditions |
| --- | --- | --- | --- |
| Nominal Voltage | V/Cell | 1.2 | Unit cell or stack-up batteries |
| Nominal Capacity | mAh | 13000 | Standard Charge/Discharge |
| Standard Charge | mA | 1300(0.1C) | T1=0~45℃(see Note1) |
|  | Hour | 14~16 |  |
| Quick Charge | mA | 3900 (0.3C) | -ΔV=0~5mV/cell or Timer Cutoff=120% nominal capacity or Temp.Cutoff=55℃, T1=10~45℃ |
|  | Hour | 4.0approx (see Note 2) |  |
| Trickle Charge | mA | (0.05C)~(0.1C) | T1=0~45℃ |
| Standard discharge | mA | 2600 (0.2C) | T1= -30~60℃ Humidity：Max.85% |
| Discharge Cut-off Voltage | V/cell | 1.0 |  |
| Storage Temperature | ℃ | -30~65 | Discharged state、Humidity、Max.85% |
| Typical Weight | Gram | 255 | Unit cell |

Document Number：　　　　　　　　　　　　　　　　　　　　　　　　　　　　　　　 Revision    3

Document Title：Product Specification of Ni-MH ESP13000FH Cells                           Page 2  of  3

4、 PERFORMANCE

Unless otherwise stated, tests should be done within one month of delivery under the following conditions：

Ambient Temperature ：20±5℃

Relative Humidity   ： 65±20%

Notes：  Standard Charge/Discharge Conditions：

Charge：   1300mA(0.1C)×14 hours

Discharge：2600 mA(0.2C) to 1.0V/cell

| Test | Unit | Specification | Conditions | Remarks |
| --- | --- | --- | --- | --- |
| Capacity | mAh | ≥13000 | Standard Charge Discharge | up to 3 cycles are allowed |
| Open Circuit Voltage(OCV) | V/cell | ≥1.25 | Within l hour after standard Charge |  |
| Internal Impedance | mΩ/cell | ≤6.5 | Upon fully charge(lKHz) |  |
| High Rate Discharge(1C) | minute | ≥54 | Standard Charge, l hour rest Before discharge by 13000mA (1C)to 1.0V/cell | up to 3 cycles are allowed |
| Overcharge | / | No leakage nor explosion | 1300mA(0.1C)Charge 28 days |  |
| Charge Retention | mAh | ≥9100(70%) | Standard Charge, Storage：28 days, Standard Discharge |  |
| IEC Cycle Life | Cycle | ≥500 | IEC285(1993)4.4.1 | (see Note 3) |
| Accelerated Cycle Life | Cycle | ≥400 | Charge:3900mA(0.3C) Discharge: 6500mA(0.5C) To 1.0V/cell, End-of:80% nominal Capacity | Cycling charging cut-off condition：-△V=0~5mV/cell and Timer cut –off=110% Nominal capacity Input and Temp.cutoff=55℃ |
| Leakage |  | No leakage nor deformation | Fully charged at :3900mA(0.3C) for 4.0 hrs Stand for 14 days |  |
| Vibration Resistance |  | Change of voltage should be under 0.02V/cell,Change of impedance should be under 5 milli-ohm/cell | Charge the battery 0.1C 14hrs,then leave for 24hrs,check battery before/after vibration, amplitude 1.5mm Vibration 3000 CPM Any direction for 60mins. |  |
| Impact Resistance |  | Change of voltage sho-uld be under 0.02V/cell Change of impedance should be under 5 milli-ohm/cell | Charge the battery 0.1C 14hrs Then leave for 24hrs,check bat-before/after dropped, Height 50cm Wooden board(thickness 30mm) Direction not specified,3 times. |  |

Document Number： 　　　　　　　　　　　　　　　　　　　　　　　　　　　　      Revision:3

Document Title：Product Specification of Ni-MH ESP13000FH Cells                              Page 3 of 3

5、CONFIGURATION, DIMENSIONS AND MARKINGS

Please refer to the attached drawing.

6、EXTERNAL APPEARANCE

The cell/battery shall be free from cracks, scars, breakage, rust, discoloration, leakage nor deformation.

7、WARRANTY

One year limited warranty against workmanship and material defects.

8、CAUTION

⑴Reverse charging is not acceptable.

⑵Charge before use. The cells/batteries are delivered in an uncharged state.

⑶Do not charge/discharge with more than our specified current.

⑷Do not short circuit the cell/battery Permanent damage to the cell/battery may result.

⑸Do not incinerate or mutilate the cell/battery.

⑹Do not solder directly to the cell/battery.

⑺the life expectancy may be reduced if the cell/battery is subjected adverse conditions like: extreme temperature, deep cycling, excessive overcharge/ over-discharge.

⑻store the cell/battery uncharged in a cool dry place. Always discharge batteries before bulk storage or shipment.

Notes：

⑴ T1: Ambient Temperature.

⑵ Approximate charge time from discharged state, for reference only.

⑶ IEC285(1993)4.4.1 Cycle Life:

| Cycle No. | Charge | Rest | Discharge |
| --- | --- | --- | --- |
| 1 | 0.1C×16h | None | 0.25C×2h20min |
| 2-48 | 0.25C×3h10min | None | 0.25C×2h20min |
| 49 | 0.25C×3h10min | None | 0.25C to 1.0V/cell |
| 50 | 0.1C×16h | 1-4h | 0.2C to 1.0V/cell |
| Cycles l to so shall be repeated until the discharge duration on any 50th Cycle becomes less than 3 h. |  |  |  |

PAGE 4

MODEL No: ESP13000FH                            Description:13000mAh F SIZE NI-MH

| Specification 32.3±0.2 10.0±0.05 89.0±0.5 with tube | 32.5±0.2 89.0±0.5 with tube |
| --- | --- |

| Nominal Capacity |  |  | 13000 mAh |
| --- | --- | --- | --- |
| Nominal Voltage |  |  | 1.2 V |
| Charge current |  | Standard | 1300mA |
|  |  | Quick | 3900 mA |
| Charge time |  | Standard | 14~16 Hrs |
|  |  | Quick | 4.0 Hrs |
| Ambient Temperature | Charge | Standard | 0℃~45℃ |
|  |  | Quick | 10℃~45℃ |
|  | Discharge |  | -30℃~60℃ |
|  | Storage |  | -30℃~65℃ |
| Internal Impedance(mΩ) (After Charge) |  |  | Max≤6.5 |
| Weight |  |  | 255g |

.

MODEL No: ESP13000FH                           Description:13000mAh F SIZE NI-MH

| Specification 32.3±0.2 8.0±0.05 90.5±0.5 with tube | 32.5±0.2 89.0±0.5 with tube |
| --- | --- |

| Nominal Capacity额定容量 |  |  | 13000 mAh |
| --- | --- | --- | --- |
| Nominal Voltage额定电压 |  |  | 1.2 V |
| Charge current 充电电流 |  | Standard标准 | 1300mA |
|  |  | Quick快充 | 3900 mA |
| Charge time 充电时间 |  | Standard标准 | 14~16 Hrs |
|  |  | Quick快充 | 4.0 Hrs |
| Ambient Temperature 使用温度 | Charge 充电 | Standard标准 | 0℃~45℃ |
|  |  | Quick快充 | 10℃~45℃ |
|  | Discharge放电 |  | -30℃~60℃ |
|  | Storage储存 |  | -30℃~65℃ |
| Internal Impedance(mΩ) (After Charge)充电后内阻 |  |  | Max≤6.5 |
| Weight重量 |  |  | 255g |