SPECIFICATIONS：

| Type | # Sealed Ni-MH Prismatic Battery cell |
| --- | --- |
| Size | ESP500PH |
| Mode | 3/5F6S |
| Nominal Voltage | 1.2V |
| Nominal Capacity | 500mAh |
| Typical Internal Impedance(at 1 kHz ) |  |
| (fully charged at 20℃max) | 35mΩ |
| Average Weight | 12.5g |
| Dimensions(including PVC tube) |  |
| Height(h) | 34.0-1.0mm |
| Width(W): | 16.0-1.0mm |
| Thickness(t): | 6.0-0.7mm |
| Capacity (20℃0.2C discharge to 1.0V) (Reference only) |  |
| Typical Capacity: | 500 mAh |
| Minimum Capacity | 450 mAh |
| Charging Method:（20℃） |  |
| Standard Charge: | Charge with 50 mA for 12 |
| Quick Charge | Charge with 150 mA for 5 hours |
| Fast Charge: | Charge with 500 mA for 72 minutes （Under -△V controlled 10mV/cell） |
| Max Overcharge Current | 50 mA(No longer than 100 hours) |
| Trickle Current | 15~25mA |
| Operating Temperature(reference only): |  |
| Storage | -20℃～+35℃ |
| Discharge: | -20℃～+60℃ |
| Standard Charge | 0℃～+45℃ |
| Fast Charge | +10℃～+45℃ |

1,Performance

| Testing Item | Testing Conditions | Standard |
| --- | --- | --- |
| Standard Testing Condition | If not specially described, Temperature 20+/-5℃ Relative Humidity:≤60%。 |  |
| - Standard Charge | 0.2C discharge to1.0V/cell,then 0.1C charge for 16 hours(Constant Current) |  |
| (2)Fast Charge | 0.2C discharge to1.0V/cell,then 0.1C charge for 72 minutes (Constant Current) |  |
| (3)Open Circuit Voltage | Test within 14 days after standard charge | ≥1.25V/cell |
| (4)Nominal Capacity | Have 30 minutes of rest after standard charge,then 0.2C discharge to 1.0V/cell 3 cycles permitted | ≥300minutes |
| (5)High Rate Discharging Capacity | Have 30 minutes of rest after fast charge, Then 1.0C discharge to 1.0V/cell,3 cycles permitted | ≥54 minutes |
| (6)Cycle Life | 0.2C Charge for 7.5 hours, have 30 minutes rest,then 0.2C discharge to 1.0V/cell,for 3 cycles,then rest as following condition: 0.5C charge for 1.2 hours,30 minutes rest; 0.5C discharge to 1.0V/cell,30 minutes rest. | 60% nominal capacity can be attained at the 300 th cycle |
|  | 2）for GB/T 15100.2-2003/IEC61951-2：2003(7.4.1.1) | ≥500 th cycle |
| (7)Over-charge | After(4) testing, 0.1C charge for 48 hours, check cell surface,0.2C discharge to 1.0V/cell. | No deformation or leakage can be found,and ≥270 minutes. |
| (8)Over-Discharge | After(4) testing, 0.2C discharge for 24 hours,under constant impedance, then standard charge,rest for 30 minutes,0.2C discharge to 1.0V /cell. | ≥240 minutes |
| (9)Temperature | Fast charged as (2) under 20+/-5℃,stored 3 hours,under followimg temperatures,then discharge to 1.0V/cell: - Discharging Temperature: 0℃ b)Discharging Temperature: 20℃ c)Discharging Temperature: 40℃ | Discharging Time 45 minutes 50 minutes 45 mimutes |
|  | Fast charged as (2) under following temperature,stored 3 hours under 20+/-5℃ , then 0.5C discharged to 1.0V/cell: a) Charging Temperature: 0℃ b)Charging Temperature: 20℃ c) Charging Temperature: 40℃ | Discharging Time 45 minutes 50 minutes 45 mimutes |
| (10)Self-discharge | After standard charge, stored for 30 days under 20+/-5℃,then discharged to 1.0V/cell | Discharging Time ≥225 minutes |
| (11)Storage | Charged or discharged as (1) condition and stored for 180 days under 20+/-5℃,then tested as(4) condition | Discharging Time ≥280 minutes |
| (12)Humidity | Standard charged and stored under RH of 60%. | No deformation or leakage found |
| (13)Vibration | Vibration in any direction at amplitude of 4 mm and A frequency of 1000 cycles per minute and continue for 60 minutes. | The battery shall conform electrical spec, mechanical deformation or damage is acceptable |
| (14)Drop | The battery shall be subjcted to drop from the height of 100cm to an oak board more than 10mm thick,the test should be carried for 3 times at each direction of the battery axis. |  |
| (15)Safety | (1)External short:Fast Charged and then short-circuited between terminals of the battery by the lead wire with the cross section area of 0.75 square millimeter. | The battery shall not explode,but electrolyte leakage or deformation of the battery is acceptable. |
|  | (2)Over charge: Charge for 5 hours at the constant current of 0.5C. |  |
|  | (3)Reverse charge: Reverse charge for 5 hours at the constant current of 0.5C. |  |
|  | (4)Safety vent operation: The reverse-charge is conducted for 30 minutes at the constant current of 1.0C.after pre-discharge at the constant current of 0.2C up to the end voltage of 0V/Cell. | Safety vent shall operate,The battery shall not explode, electrolyte leakage or deformation of the battery is acceptable. |

2．Note:

1).Do not dispose of cell into fire or be dismantled under any condition.

2).Do not mix different cell types and capacities in the same battery assembly.

3).Charge and discharge under specified ambient temperature recommended  to BFN

specification.

4).Short circuit leading to cell venting must be avoided .

5).Never solder onto cell directly.

6).Cell reversal should be avoided.

7).Use batteries in extreme condition may affect the service life, such as:extreme temperature, deep cycle,extreme overhcarge and over discharge.

8).Batteries should be stored in a cool dry place.

9).Once problems be found,stop using,send batteries to local dealer.

3,Storage

1).It is strongly recommended to store Ni-MH batteries and cells in the temperature range from -20

to 25℃ ,and in low humidity and no corrosive gas environment,to maintain a reasonably high

capacity recovery level.

2). Avoid storage higher (e.g.35℃),lower temperature than –20℃ ,or higher humidity which would result in deterioration or damage to the cells and batteries such as follows:

4, Permanent capacity loss

Electrolyte leakage resulted from the expansion or shrinkage of organic material inside the cells

5, Rust of metal parts.

6, Up to three full cycles of charge /discharge after long-termed storage may need to obtain highest

capacity.

GB/T 15100.2-2003/IEC61951-2：2003(7.4.1.1) Endurance in cycles

| Cycle number | Charge | Stand in charged condition | Discharge |
| --- | --- | --- | --- |
| 1 | 0.1CA (50mA) for 16h | none | 0.25CA (125mA) for 2h 20 min |
| 2-48 | 0.25CA (125mA) for 3h 10 min | none | 0.25CA (125mA) for 2h 20 min |
| 49 | 0.25CA (125mA) for 3h 10 min | none | 0.25CA (125mA) to 1.0 V |
| 50 | 0.1CA (50mA) for 16h | 1 h to 4 h | 0.2CA (100mA) to 1.0 V |

Cycle 1 to 50 shall be repeated until the discharge duration on any 50th cycle becomes Less than

3 h. At this stage, a repeat capacity measurement as specified for cycle 50 shall be carried out.

The endurance test is considered complete when two successive capacity measurement cycles give a discharge duration of less than 3 h. The number of cycles obtained when the test is completed shall be not less than 500.